Thinner GP:-

GP Thinner is a low cost blend for acrylic and nitrocellulose lacquers, some enamels and

cleaning and for thinning Flexiprime, FM1 Auto Primer and Grille Black.

Product Type: Clear Liquid

Density: 0.830 kg/L

Recommended DFT: 25-35 microns DFT /coat

Theoretical Coverage:8m²/L @ 40 Microns DFT / spray equipment dependant.

Properties VOC: 742 g/L

Boiling point: 50°C

Sizes: 1L, 4L, 20L, 60L, 208L

Dangerous Goods: 3A

UN: 1263

Hazchem: 3(Y)E

Packing Group: II

Shipment name: PAINT Related Material (Flammable)

Flash point: < 23°C

 